# DNA-origami functionalized with metal nanoparticles

Alla Nykytenko, Antti-Pekka Eskelinen*, Christian Leiterer, Andrea Csáki, Päivi Törmä*, Wolfgang Fritzsche

Institute of Photonic Technology, Albert-Einstein-Str. 9, 07745 Jena, Germany

* Aalto University School of Science and Technology, P.O.Box 15100, FI-00076 AALTO, Finland

DNA-origami is prepared using long single-stranded DNA molecules folded into arbitrary 2D-planar nanostructures utilizing various short helper strands as clamps. It represents a self-assembling of 90 x 90 nm objects with roughly 6 nm resolution from the 7 kilobase single-stranded genomic DNA of M13mp18 (Fig. 1) [1,2]. We can carry out different methods of functionalizations of gold, silver, core-shell, silica, and magnetic nanoparticles, and would like to combine these particles with the DNA super structure. A result is shown in (Fig. 2). This image demonstrates that the integration of gold nanoparticles functionalized with DNA to the surface of the “smiley” origami structure could be accomplished using gold nanoparticles of different sizes. We compared different conjugations with 5, 12 and 30 nm gold nanoparticles. They are stable under hybridization up to 60°C. Finally, we showed that the addition of specific attachment gold nanoparticles conjugated smiley’s to the electrodes during dielectrophoresis (Fig. 3).

Possible applications of this technology for the precise combination of metal nanoparticles with DNA superstructures are expected in nanoelectronics and nanophotonics.

Funding by the DAAD (PPP [50020468]) and from ProExzellenz [113-1] is gratefully acknowledged.

| Fig. 1: “Smiley” DNA origami structure adsorbed onto mica substrate | Fig. 2: Origami structure with nanoparticles (12 nm, gold) attached using 5'-thiol modified oligonucleo-tides | Fig. 3: Origami structure positioned on the micro electrode gap by dielectrophoresis |
| --- | --- | --- |

[1] N. C. Seeman, Nature 421 (2003) 427-431. T. H. LaBean and H. Li, Nano Today 2 (2007) 26-35.

[2] P. W. K. Rothemund, Nature 440 (2006) 297-302.

[3] A. Kuzyk et al., Nanotechnology 20, 235305 (2009).